# MHD effects on turbulence

Example:

## Flibe flow in a FW coolant channel in a magnetic field (3 orientations)

- Velocity: U=5 m/s, 10 m/s, 15 m/s

- Channel dimension (half-width): b=1 cm

- Non-conducting walls: cw=0

- Heat flux:qw=1 Mw/m2

- Channel length: L=8 m

MHD effects on turbulence (cont.)

Calculations based on the k-epsilon model for MHD turbulence

MHD effects on turbulence (cont.)

Wall-normal magnetic field, U=5 m/s, b=1 cm

MHD effects on turbulence (cont.)

(T=Tw-l-Tb in the reference Flibe flow

| Case No | BWall-normal | BSpanwise | B Streamwise |
| --- | --- | --- | --- |
| 1: U=5 m/s, B=0 | 127.1 | 127.1 | 127.1 |
| 2: U=5 m/s, B=5 T | 135.9 | 131.1 | 127.1 |
| 3: U=5 m/s, B=10 T | 175.5 | 143.7 | 127.3 |
| 4: U=10 m/s, B=0 | 67.4 | 67.4 | 67.4 |
| 5: U=10 m/s, B=5 T | 69.3 | 68.2 | 67.4 |
| 6: U=10 m/s, B=10 T | 75.5 | 70.9 | 67.5 |
| 7: U=15 m/s, B=0 | 46.6 | 46.6 | 46.6 |
| 8: U=15 m/s, B=5 T | 47.4 | 46.9 | 46.6 |
| 9: U=15 m/s, B=10 T | 49.8 | 48.1 | 46.6 |

MHD effects on turbulence (cont.)

Concerns arisen by M.Abdou after reviewing the calculations

- What is a reasonable velocity? Must be discussed and answered during the Meeting.

- We need an upgraded database with material properties, since the data for Flibe tend to be controversial.

- What is the effect of conducting walls on turbulence? How can we evaluate this effect?

- How can we verify the calculations?

- What do we need in the experiment (JII)? What experimental conditions do we need in order to observe the effect of MHD on turbulence?

# Text boxes

Heat flux

2b

L

Flow

Turbulence reduction and heat transfer degradation in Flibe: wall-normal magnetic field, U=5 m/s, b=1 cm

Nusselt number

Temperature rise

Physical properties at t=500(C (table 7.3-1, APEX Interim Report)

(=2050 kg/m3

(=7.4(10-6 m2/s

(=155 1/Ohm-m

k=1.06 W/m-K

Cp=2380 J/kg-K

Turbulence reduction and heat transfer degradation in Flibe: wall-normal magnetic field, U=5 m/s, b=1 cm