IEA Liquid Breeder Workshop

Dai-Kai Sze, UCSD

Presented at the

US TBM Meeting

UCLA, May 10-11, 2006

IEA Sub Task on Liquid Breeders

# The key persons on the IEA sub task on liquid breeder are

Dr. Dai-Kai Sze   Chair

Dr. Luciano Giancarli

Dr. Igor Kirrilov

Professor Sataru Tanaka

# China and S Korea will also participate on the IEA collaboration.

# Plan for collaboration on liquid breeders was discussed.

Concerns on liquid breeders

# Liquid breeders collaboration is difficult because each systems are very different.

# There are high conductors, and low conductors.

# There are conducting walls, simi-insulated walls, and insulated walls.

# There are high velocity designs, moderate velocity designs, and low velocity designs.

# There are high tritium solubility, low tritium solubility breeders.

# The different combinations of design, breeder selection, structural material selection, etc, will change completely on the key issues of the blanket.

# How to select a collaboration which will fit into all the requirements from different IEA parties is a main concern.

# Discussion follow the ISFNT

- A meeting was hold at Tokyo during the ISFNT to discuss possible collaboration on liquid breeders.

- It was agreed that to develop a joint R/D program toward ITER TBM applications would be a good target for the IEA collaboration.

- It is necessary to review what are the remain R/D issues for the ITER TBM development.

- It will be useful if we can concentrate our R/D toward solve those problems.

Why International Collaboration

- There are severe limitations on the available resource for the R/D program for many of the ITER parties.

- There are severe limitations on the R/D schedule (maybe 5 years).

- The key issues associated with breeding material selection are almost independent on the blanket concept.

- International collaboration is well suite with those conditions.

An example  (based on tritium control)

- The R/D works on blanket tritium control are focused on tritium recovery and permeation barrier development.

- Tritium recovery based on LiPb/He contact is not efficient.

- Surface oxidation can significantly reduce the permeation rate.

- Permeation barrier development has not been successful, either for fusion program, or for defense program.

- Tritium control remains to be a key issue for DEMO blanket.

What needs to be done

- An efficient tritium recovery process needs to be developed.

- A reliable tritium diffusion barrier, with a consistent reduction factor, need to be developed.

- A leaking rate for the coolant system, either water or He, needs to be demonstrated.

- A Room Air Detriation System (RADS) needs to be developed.

(Control DTO is very different from control DT)

- With those information, the coolant process rate, for either He or water, can be determined.

- Tritium recovery process, from He or water, needs to be developed.

Comment

- This is a much more complicated process than just develop tritium recovery process and diffusion barrier development.

- Diffusion barrier development is difficult, and may not provide the reduction factor we will need.

- It is important to control tritium by recovery it from either water or He.

- Also, tritium recovery from the RTDS is an important step.

- We will need four or five different steps to control tritium loss.

- Reduce tritium loss to ~ 10 Ci/d needs all the effort.

Another example  (corrosion)

- The key work on corrosion was investigating temperature effect on corrosion.

- Other experimental conditions will also be important:

Effect of temperature on corrosion

Effect of velocity on corrosion

Effect of MHD on corrosion

Effect of nature convection on     corrosion

Effect of material on corrosion

Corrosion reduction

- The experimental time will be about 0.5 year per experiment (4000 hours)

- A few corrosion experimental set ups will be required to do all the work.

- It is useful for ITER parties to do the work together in collaboration.

What will we accomplish

- The key work to accomplish during the workshop is to discuss what are the critical R/D programs for the ITER TBM.

- The topics of discussion are

LiPb development

Li development

LiPb structural material issues

Li structural material issues

Tritium control special topic

MHD special topic

- The required R/D issues for those topics will be discussed and summarized.

What we will do after the workshop

- We will have internal discussion on US interest on the required R/D.

- We will also discuss what are the special R/D programs for the DCLL.

- IEA task leaders will meet again later this year to summarize the R/D proposals from each ITER TBM parties.

- The goal is to set up an coordinated R/D program for the TBM development.

What maybe the US positions

- US TBM position is not clear at this time.

- The best option is to have our independent ITER TBM design and program (DCLL).

- For this case, we will have our own complete R/D program, and will have information exchange with other ITER parties.

- We may have our own TBM (DCLL), and carried out R/D as a part of this collaboration.

- We will select a number of R/D activities, and depend other parties for other information.

- It is also possible that we will work together with other parties on TBM.

- We can contribute on key R/D areas based on our expertise.

- This decision maybe made between now and end of this year.

US position in the workshop

- The workshop will identify the required R/D on liquid breeder TBMs.

- Therefore, no US position needs to be identified before the workshop.

- After the required R/Ds are identified, we will have internal discussion on the US position.

- This position needs to be consistent with the US program on TBM, which is DCLL.

Summary

- International collaboration is necessary for the ITER TBM activities.

- IEA collaboration is a good way to start this discussion.

- The require R/D for the liquid breeder TBMs have to be identified.

- The US TBM R/D activities have to be consistent with the US TBM design, the US TBM program, and US expertise.

- A coordinated R/D program for the TBM can resolve many difficult problems for ITER parties.