# Tritium Control

# Dai-Kai Sze

# UCSD

# Presented at the

# APEX/TBM Project Meeting

# November 3-5, 2003

# UCLA

# Issues on tritium control

# Most fusion blanket has a high tritium partial pressure.

# The temperature of the blanket is high for high thermal converting efficiency.

# The surface area of HT is large, and the wall is thin.

# Those are some of the perfect conditions for tritium permeation down stream.

# The allowable tritium leakage rate is 1 Ci/FPD.

# Tritium partial pressure

# The tritium partial pressures over most of the breeding materials are very high.

# Assuming perfect tritium recovery system, the tritium partial pressures per coolant path are

# LiPb = 0.014 Pa

# Flibe = 380 Pa

# Assuming tritium concentration of 1 appm, the tritium partial pressure over Li is 2.6X10-8 Pa.

# Assuming a purge gas flow rate of 104 l/s, the tritium partial pressure in the He purge gas for solid breeder is 0.6 Pa.

# Only self-cooled Li blanket has low tritium partial pressure. All other blankets have high tritium partial pressure.

# Permeation Considerations

# Typical parameters for HX are:

# Temperature              500C

# Surface Area              2.5X104 m2

# Wall thickness           1 mm

# Allowable T leakage  1 Ci/d

# Tritium Permeability

# 0.46 (mol T2-mm/D-M2-atm0.5)

# If the allowable tritium leakage rate is 1 Ci/d, the allowable tritium partial pressure before the HX has to be 2.1X10-13 Pa!!!

# If the allowable tritium leakage is 100 Ci/d, the allowable tritium partial pressure would be 2.1X10-9 Pa. Li is getting close.

# If the allowable tritium leakage rate is 100 Ci/d, and we will have a diffusion coating with an effectiveness of 100, the allowable tritium partial pressure would be 2.1X10-5 Pa, which is still too high for LiPb, flibe and solid breeder.

# We will need the combination of efficient tritium recovery, development of diffusion coating, and also secondary recovery from secondary coolants, water or He.

# EC developed a water-cooled LiPb blanket.

# It was assumed that a diffusion coating can be developed with a reduction factor 0f 100.

# Efficient tritium recovery from LiPb was assumed.

# The tritium permeation to water was calculated to be ~ 1 g/d.

# Secondary tritium recovery from water was required to clean up the water.

# Conclusion

# Tritium control in a fusion blanket is difficult.

# The large tritium throughput, the high operating temperature, the large heat transport system, and the form of tritium (in elementary form) all compound the problem.

# This problem was identified as a common problem for IEA liquid breeder task.

# * Many steps will be required to limit the tritium loss rate to be within acceptable level.